
[image: image1.png]



Acoustical wall panel 

Content          
Demountable acoustic gypsum wall for acoustic regulation.
Laminated surface with possibility for individual surface designs.
Product can be recycled after end of life.
Products and materials

Tangent_450 x < 1200/2400 > x 9.5_B
Material: Perforated plasterboard
Board Type: Gypsum panel
Dimensions: 450 x <1200/2400> x 9.5mm

Weight: 4.0 and 8.0 kg/panel



Edge: B, mitred and glued long edges
Perforation: Obround 4x14mm holes, c/c 10/20mm.
Perforation percent: 23.9 – 24.5%

Surface: Laminated foil (PVC-free), pH resistant 2.5 - 13.0

             (Individual print design on request)

Colour: Ultra white NCS S0300-N, (RAL 9016); gloss 10
Light reflection: 74.1% in accordance with DIN 5036
Fire rating: B-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low


Acoustics 
                  55mm installation depth with 33mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.25
	0.65
	0.90
	0.90
	0.85
	0.80
	0.90
	0.85



Accessories
ADIT comes as a kit with 2xpanels and all the accessories needed.

Installation
· In accordance with included installation guide that comes along with the kit. 
