
[image: image1.png]



Acoustical deck and wall mount panels 

Content          
Impact resistant acoustic gypsum panel for ceiling and wall mount with visible white screws.
Laminated surface for easy cleaning and high hygienic needs.
Product can be recycled after end of life.
Products and materials

Globe_600 x < 1200/1800/2400 > x 12.5_B
Material: Perforated plasterboard
Board Type: Gypsum panel
Dimensions: 600 x 1200 x 12.5mm (or on request)

Weight: 8.50-9.40 kg/m²



Edge: B, bevelled edge with visible joints.
Perforation: Round 6mm holes, c/c 15mm.
Perforation percent: 10.2 %

Surface: Laminated foil (PVC-free), pH resistant 2.5 - 13.0

Colour: Ultra white NCS S0300-N, (RAL 9016); gloss 10

Hygiene: Tested for chemical resistance in accordance with DIN 68 861,

              FIRA BS 3962 and NEMA LD-3-1991.
Light reflection: 74.1% in accordance with DIN 5036
Fire rating: B-s1,d0 in accordance with EN 13501-1
Impact: Rated Class 1 in accordance with EN 13964

Indoor climate: Degasification 10 days
Particle emission: Low


Acoustics 
                  200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.65
	0.80
	0.65
	0.55
	0.45
	0.60(L)
	0.65


                  200mm suspension with 50mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.55
	0.75
	0.75
	0.60
	0.60
	0.55
	0.65
	0.70


Wall connection

Type: UD-profile

Material: 0.60mm galvanized steel

Dimension: Width 28mm | Height 27mm | Length 3000mm
Primary profile
Type: CD-profile
Material: 0.60mm galvanized steel
Dimensions: Width 60mm | Height 27mm | Length 3000mm

Secondary profile
Type: CD-profile
Material: 0.60mm galvanized steel
Dimensions: Width 60mm | Height 27mm | Length 3000mm

Suspension

Type: Nonius hanger lower part

Type: Nonius hanger upper part


Dimension: < xxx - xxx mm >

Type: Split pin for hanger

Accessories

Type: Length connector for CD-profile


Dimension: Width 58mm | Height 28mm | Length 80mm

Type: Cross-fitting for primary and secondary profile

Type: WS Screws
Dimension: 
<WS25S white 25mm – for 1 layer on steel>


<WS38S white 38mm – for 2 layer on steel>

<WS32T white 32mm – for 1 layer on wood>


<Nr.408 white 42mm – for 2 layer on wood>

Installation
· Screw spacing for attachment of wall connections max. 400mm c/c and in relation to the required ceiling height < xxx mm > (min: 80mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 900 mm.
· Distance between hangers ≤ 900 mm.
· Distance from wall to first load-bearing (primary profile) section ≤ 200 mm.
· Distance between load-bearing (Primary profile) sections ≤ 900 mm.

· Distance between secondary profiles is Max. 200mm (max. 300mm if no impact requirements are needed).
· Mount the acoustic gypsum panel crosswise (red against blue marking) on the secondary profile and with a screw fixing distance at max. c/c 200mm (max. 300mm if no impact requirements are needed). Or in accordance with included template or screw placement. 
[image: image2.png]



Acoustical deck and wall mount panels 

Content          

Impact resistant acoustic gypsum panel for ceiling and wall mount with visible white screws.

Laminated surface for easy cleaning and high hygienic needs.
100% recyclable product.    

Products and materials

Regula_600 x < 1200/1800/2400 > x 12.5_B
Material: Non-perforated plasterboard

Board Type: Gypsum panel
Dimensions: 600 x 1200 x 12.5mm (or on request)

Weight: 8.50-9.40 kg/m²



Edge: B, bevelled edge with visible joints.
Surface: Laminated foil (PVC-free), pH resistant 2.5 - 13.0

Colour: Ultra white NCS S0300-N, (RAL 9016); gloss 10

Hygiene: Tested for chemical resistance in accordance with DIN 68 861,

              FIRA BS 3962 and NEMA LD-3-1991.

Light reflection: 86.3% in accordance with DIN 5036
Fire rating: B-s1,d0 in accordance with EN 13501-1

Impact: Rated Class 1 in accordance with EN 13964

Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 

All suspension without mineral wool


	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.20
	0.10
	0.05
	0.05
	0.05
	0.10
	0.05


Wall connection

Type: UD-profile

Material: 0.60mm galvanized steel

Dimension: Width 28mm | Height 27mm | Length 3000mm
Primary profile
Type: CD-profile
Material: 0.60mm galvanized steel
Dimensions: Width 60mm | Height 27mm | Length 3000mm

Secondary profile
Type: CD-profile
Material: 0.60mm galvanized steel
Dimensions: Width 60mm | Height 27mm | Length 3000mm

Suspension

Type: Nonius hanger lower part

Type: Nonius hanger upper part


Dimension: < xxx - xxx mm >

Type: Split pin for hanger

Accessories

Type: Length connector for CD-profile


Dimension: Width 58mm | Height 28mm | Length 80mm

Type: Cross-fitting for primary and secondary profile

Type: WS Screws
Dimension: 
<WS25S white 25mm – for 1 layer on steel>


<WS38S white 38mm – for 2 layer on steel>

<WS32T white 32mm – for 1 layer on wood>


<Nr.408 white 42mm – for 2 layer on wood>

Installation
· Screw spacing for attachment of wall connections max. 400mm c/c and in relation to the required ceiling height < xxx mm > (min: 80mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 900 mm.
· Distance between hangers ≤ 900 mm.
· Distance from wall to first load-bearing (primary profile) section ≤ 200 mm.
· Distance between load-bearing (Primary profile) sections ≤ 900 mm.

· Distance between secondary profiles is Max. 200mm (max. 300mm if no impact requirements are needed).
· Mount the acoustic gypsum panel crosswise (red against blue marking) on the secondary profile and with a screw fixing distance at max. c/c 200mm (max. 300mm if no impact requirements are needed). Or in accordance with included template or screw placement. 
