
[image: image1.png]



Demountable acoustic ceiling

Content          
Demountable acoustic gypsum ceiling for concealed T-grid system.
Repaintable without loss of acoustics. 
Product can be recycled after end of life.
Suitable as ventilation ceiling with concealed air inlet.    

Products and materials

Unity 3_600 x 600 x 12.5_D+
Material: Perforated plasterboard
Board Type: Ceiling tile
Dimensions: 600x600x12.5mm

Weight: 9.20-9.90 kg/m²



Edge: D+, concealed T-grid system.
Perforation: Square 3.5x3.5mm holes, c/c 8.33mm, Perforation to edge.
Perforation percent: 17.2 %

Surface: Water-based acrylic paint
Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 69.2% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low


Acoustics 

200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.50
	0.80
	0.85
	0.75
	0.75
	0.80
	0.80
	0.80


                  200mm suspension with 45mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.60
	0.90
	0.90
	0.85
	0.85
	0.85
	0.90
	0.90


Main runner
Type: T-profile
Material: 0.4mm galvanized steel
Colour: White
Dimensions: Width 24mm | Height 38mm

Spacer bar

Type: V-profile
 
Material: Galvanized steel
Dimensions: Length 600mm
Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.5mm galvanized steel

Colour: White
Dimension: < 24x20mm or 19+11 x 13+19mm >


Suspension

Type: < Adjustable hanger or direct hanger >

Dimension: < xxx - xxx mm >
Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 63mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 100 mm.
· Distance between hangers ≤ 1500 mm.
· Distance from wall to first load-bearing (main runner) section ≤ 600 mm.
· Distance between load-bearing (main runner) sections ≤ 600 mm.

· Align the first load-bearing (main runner) along one of the walls and secure it with help of adjusted spacer bar fixed into the wall.
When first load-bearing (main runner) are aligned, then install the other spacer bars.
· Units of up to 1.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.
[image: image2.png]


Demountable acoustic ceiling 


Content          

Demountable acoustic gypsum ceiling for concealed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.    


Suitable as ventilation ceiling with concealed air inlet.    
Products and materials

Unity 4_600 x 600 x 12.5_D+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm

Weight: 9.20-9.90 kg/m²



Edge: D+, concealed T-grid system.
Perforation: Round 4mm holes, c/c 10mm, Perforation to edge.

Perforation percent: 12.2 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 72.5% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.75
	0.80
	0.70
	0.65
	0.60
	0.70
	0.75


                  200mm suspension with 45mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.55
	0.80
	0.80
	0.75
	0.75
	0.65
	0.75
	0.80


Main runner
Type: T-profile
Material: 0.4mm galvanized steel
Colour: White 

Dimensions: Width 24mm | Height 38mm

Spacer bar

Type: V-profile
 
Material: Galvanized steel
Dimensions: Length 600mm

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.5mm galvanized steel

Colour: White
Dimension: < 24x20mm or 19+11 x 13+19mm >



Suspension

Type: < Adjustable hanger or direct hanger >

Dimension: < xxx - xxx mm >
Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 63mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 100 mm.
· Distance between hangers ≤ 1500 mm.
· Distance from wall to first load-bearing (main runner) section ≤ 600 mm.
· Distance between load-bearing (main runner) sections ≤ 600 mm.

· Align the first load-bearing (main runner) along one of the walls and secure it with help of adjusted spacer bar fixed into the wall.
When first load-bearing (main runner) are aligned, then install the other spacer bars.
· Units of up to 1.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.

[image: image3.png]


Demountable acoustic ceiling 


Content          

Demountable acoustic gypsum ceiling for concealed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.    


Suitable as ventilation ceiling with concealed air inlet.    
Products and materials

Unity 6_600 x 600 x 12.5_D+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm

Weight: 9.20-9.90 kg/m²



Edge: D+, concealed T-grid system.
Perforation: Round 6mm holes, c/c 15mm, Perforation to edge.

Perforation percent: 11.9 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 72.8% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.60
	0.70
	0.65
	0.60
	0.60
	0.65
	0.60


                  200mm suspension with 45mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.60
	0.75
	0.70
	0.65
	0.60
	0.70
	0.70


Main runner
Type: T-profile
Material: 0.4mm galvanized steel
Colour: White 

Dimensions: Width 24mm | Height 38mm

Spacer bar

Type: V-profile
 
Material: Galvanized steel
Dimensions: Length 600mm

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.5mm galvanized steel

Colour: White

Dimension: < 24x20mm or 19+11 x 13+19mm >



Suspension

Type: < Adjustable hanger or direct hanger >

Dimension: < xxx - xxx mm >
Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 63mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 100 mm.
· Distance between hangers ≤ 1500 mm.
· Distance from wall to first load-bearing (main runner) section ≤ 600 mm.
· Distance between load-bearing (main runner) sections ≤ 600 mm.

· Align the first load-bearing (main runner) along one of the walls and secure it with help of adjusted spacer bar fixed into the wall.
When first load-bearing (main runner) are aligned, then install the other spacer bars.
· Units of up to 1.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.
[image: image4.png]


Demountable acoustic ceiling 


Content          

Demountable acoustic gypsum ceiling for concealed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.    


Suitable as ventilation ceiling with concealed air inlet.    
Products and materials

Unity 8|15|20_600 x 600 x 12.5_D+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm

Weight: 9.20-9.90 kg/m²



Edge: D+, concealed T-grid system.
Perforation: Random round 5|8|15|20mm holes, Perforation to edge.

Perforation percent: 10.8 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 72.2% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.55
	0.60
	0.60
	0.50
	0.50
	0.60
	0.55


                  200mm suspension with 45mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.60
	0.55
	0.60
	0.55
	0.60
	0.60
	0.55


Main runner
Type: T-profile
Material: 0.4mm galvanized steel
Colour: White
Dimensions: Width 24mm | Height 38mm

Spacer bar

Type: V-profile
 
Material: Galvanized steel
Dimensions: Length 600mm

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.5mm galvanized steel

Colour: White
Dimension: < 24x20mm or 19+11 x 13+19mm >



Suspension

Type: < Adjustable hanger or direct hanger >

Dimension: < xxx - xxx mm >
Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 63mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 100 mm.
· Distance between hangers ≤ 1500 mm.
· Distance from wall to first load-bearing (main runner) section ≤ 600 mm.
· Distance between load-bearing (main runner) sections ≤ 600 mm.

· Align the first load-bearing (main runner) along one of the walls and secure it with help of adjusted spacer bar fixed into the wall.
When first load-bearing (main runner) are aligned, then install the other spacer bars.
· Units of up to 1.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.
[image: image5.png]


Demountable acoustic ceiling

Content          

Demountable acoustic gypsum ceiling for concealed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.    


Suitable as ventilation ceiling with concealed air inlet.    
Products and materials

Unity 9_600 x 600 x 12.5_D+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm

Weight: 9.20-9.90 kg/m²



Edge: D+, concealed T-grid system.
Perforation: Square 9x9mm holes, c/c 20mm, Perforation to edge.

Perforation percent: 18.9 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 71.6% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.75
	0.85
	0.75
	0.75
	0.65
	0.75
	0.80


                  200mm suspension with 45mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.55
	0.85
	0.85
	0.80
	0.85
	0.80
	0.85
	0.85


Main runner
Type: T-profile
Material: 0.4mm galvanized steel
Colour: White
Dimensions: Width 24mm | Height 38mm

Spacer bar

Type: V-profile
 
Material: Galvanized steel
Dimensions: Length 600mm

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.5mm galvanized steel

Colour: White
Dimension: < 24x20mm or 19+11 x 13+19mm >



Suspension

Type: < Adjustable hanger or direct hanger >

Dimension: < xxx - xxx mm >
Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 63mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 100 mm.
· Distance between hangers ≤ 1500 mm.
· Distance from wall to first load-bearing (main runner) section ≤ 600 mm.
· Distance between load-bearing (main runner) sections ≤ 600 mm.

· Align the first load-bearing (main runner) along one of the walls and secure it with help of adjusted spacer bar fixed into the wall.
When first load-bearing (main runner) are aligned, then install the other spacer bars.
· Units of up to 1.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.
[image: image6.png]


Demountable acoustic ceiling

Content          

Demountable acoustic gypsum ceiling for concealed T-grid system.
100% recyclable product.    

Products and materials

Regula_600 x 600 x 12.5_D+
Material: Non-perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm

Weight: 9.20-9.90 kg/m²



Edge: D+, concealed T-grid system.
Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 82.6% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low


Acoustics 

All suspension without mineral wool


	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.20
	0.10
	0.05
	0.05
	0.05
	0.10
	0.05


Main runner
Type: T-profile
Material: 0.4mm galvanized steel
Colour: White 

Dimensions: Width 24mm | Height 38mm

Spacer bar

Type: V-profile
 
Material: Galvanized steel
Dimensions: Length 600mm

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.5mm galvanized steel

Colour: White
Dimension: < 24x20mm or 19+11 x 13+19mm >



Suspension

Type: < Adjustable hanger or direct hanger >

Dimension: < xxx - xxx mm >
Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 63mm)
· Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 100 mm.
· Distance between hangers ≤ 1500 mm.
· Distance from wall to first load-bearing (main runner) section ≤ 600 mm.
· Distance between load-bearing (main runner) sections ≤ 600 mm.

· Align the first load-bearing (main runner) along one of the walls and secure it with help of adjusted spacer bar fixed into the wall.
When first load-bearing (main runner) are aligned, then install the other spacer bars.
· Units of up to 1.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.
