
[image: image1.png]



Demountable self-supported acoustic ceiling 

Content          
Demountable self-supported acoustic gypsum ceiling for easy access.
Repaintable without loss of acoustics. 
Product can be recycled after end of life.    

Products and materials

Micro_400 x < 1200/1800/2400 > x 9.5_D
Material: Perforated plasterboard
Board Type: Ceiling tile
Dimensions: 400 x < 1200/1800/2400> x 9.5mm (or on request)

Weight: 11.66-12.69 kg/m²



Edge: D, visible trim at short ends
Perforation: Square 3x3mm holes, c/c 8.33mm.
Perforation percent: 10.6 %

Surface: Water-based acrylic paint
Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 72.1% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low


Acoustics 

200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.55
	0.65
	0.60
	0.60
	0.55
	0.65
	0.60


                  200mm suspension with 50mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.70
	0.75
	0.75
	0.75
	0.75
	0.75
	0.75


Reinforcement profile
Type: Flex-profile
Material: galvanized steel
Dimensions: Width 66mm | Height 44mm | length <1194/1794/2394mm>
Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.7mm galvanized steel

Colour: White (RAL 9016)
Dimension: < 20x40mm or 20x20x20x20mm >


Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 80mm with shadow line trim or min 300mm with L-profile)
· Mount the flex-profiler on the backside of the ceiling tile sliding it over the gypsum strip with two cut-rails. 
· Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², independently reinforcement or support must be used.
[image: image2.png]



Demountable self-supported acoustic ceiling

Content          

Demountable self-supported acoustic gypsum ceiling for easy access.
Repaintable without loss of acoustics. 
100% recyclable product.    

Products and materials

Globe_400 x < 1200/1800/2400 > x 9.5_D
Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 400 x < 1200/1800/2400> x 9.5mm (or on request)

Weight: 11.66-12.69 kg/m²



Edge: D, visible trim at short ends
Perforation: Round 6mm holes, c/c 15mm.
Perforation percent: 10.6 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 72.8% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.65
	0.80
	0.65
	0.55
	0.45
	0.60
	0.65


                  200mm suspension with 50mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.55
	0.80
	0.80
	0.65
	0.60
	0.55
	0.65
	0.70


Reinforcement profile
Type: Flex-profile
Material: galvanized steel
Dimensions: Width 66mm | Height 44mm | length <1194/1794/2394mm>

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.7mm galvanized steel

Colour: White
Dimension: < 20x40mm or 20x20x20x20mm >


Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 80mm with shadow line trim or min 300mm with L-profile)
· Mount the flex-profiler on the backside of the ceiling tile sliding it over the gypsum strip with two cut-rails. 
· Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², independently reinforcement or support must be used.
[image: image3.png]


Demountable self-supported acoustic ceiling

Content          

Demountable self-supported acoustic gypsum ceiling for easy access.
Repaintable without loss of acoustics. 
100% recyclable product.    

Products and materials

Quadril_400 x < 1200/1800/2400 > x 9.5_D
Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 400 x < 1200/1800/2400> x 9.5mm (or on request)

Weight: 11.66-12.69 kg/m²



Edge: D, visible trim at short ends
Perforation: Square 12mm holes, c/c 15mm.
Perforation percent: 14.2 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 75.1% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.60
	0.70
	0.65
	0.60
	0.45
	0.60
	0.65


                  200mm suspension with 50mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.55
	0.80
	0.85
	0.75
	0.70
	0.60
	0.75
	0.80


Reinforcement profile
Type: Flex-profile
Material: galvanized steel
Dimensions: Width 66mm | Height 44mm | length <1194/1794/2394mm>

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.7mm galvanized steel

Colour: White (RAL 9016)

Dimension: < 20x40mm or 20x20x20x20mm >


Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 80mm with shadow line trim or min 300mm with L-profile)
· Mount the flex-profiler on the backside of the ceiling tile sliding it over the gypsum strip with two cut-rails. 
· Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², independently reinforcement or support must be used.
[image: image4.png]


Demountable self-supported acoustic ceiling

Content          

Demountable self-supported acoustic gypsum ceiling for easy access.
Repaintable without loss of acoustics. 
100% recyclable product.    

Products and materials

Tangent_400 x < 1200/1800/2400 > x 9.5_D
Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 400 x < 1200/1800/2400> x 9.5mm (or on request)

Weight: 11.66-12.69 kg/m²



Edge: D, visible trim at short ends
Perforation: Obround 4x14mm holes, c/c 10/20mm.

Perforation percent: 21.3 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 70.9% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


200mm suspension without mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.45
	0.65
	0.80
	0.75
	0.75
	0.75
	0.80
	0.75


                  200mm suspension with 50mm mineral wool

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.75
	0.95
	0.95
	0.90
	0.90
	0.95
	0.95
	0.95


Reinforcement profile
Type: Flex-profile
Material: galvanized steel
Dimensions: Width 66mm | Height 44mm | length <1194/1794/2394mm>

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.7mm galvanized steel

Colour: White (RAL 9016)

Dimension: < 20x40mm or 20x20x20x20mm >


Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 80mm with shadow line trim or min 300mm with L-profile)
· Mount the flex-profiler on the backside of the ceiling tile sliding it over the gypsum strip with two cut-rails. 

· Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², independently reinforcement or support must be used.
[image: image5.png]


Demountable self-supported acoustic ceiling

Content          

Demountable self-supported acoustic gypsum ceiling for easy access.
100% recyclable product.    

Products and materials

Regula_400 x < 1200/1800/2400 > x 9.5_D
Material: Non-perforated plasterboard

Board Type: Ceiling tile

Dimensions: 400 x < 1200/1800/2400> x 9.5mm (or on request)

Weight: 11.66-12.69 kg/m²



Edge: D, visible trim at short ends
Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 82.6% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low

Acoustics 


All suspension without mineral wool


	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.20
	0.10
	0.05
	0.05
	0.05
	0.10
	0.05


Reinforcement profile
Type: Flex-profile
Material: galvanized steel
Dimensions: Width 66mm | Height 44mm | length <1194/1794/2394mm>

Wall connection

Type: < L-profile or Shadow line trim>

Material: 0.7mm galvanized steel

Colour: White (RAL 9016)

Dimension: < 20x40mm or 20x20x20x20mm >


Installation
· Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 80mm with shadow line trim or min 300mm with L-profile)
· Mount the flex-profiler on the backside of the ceiling tile sliding it over the gypsum strip with two cut-rails. 

· Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², independently reinforcement or support must be used.

