
[image: image1.png]



Acoustical deck and wall mount panels 

Content          
Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
Product can be recycled after end of life.
Products and materials

Micro_<900x2700> or < 1200x2400 > x 12.5_B1
Material: Perforated plasterboard
Board Type: Gypsum panel
Dimensions: <900x2700x12.5mm> or <1200x2400x12.5mm>

Weight: 9.20-9.90 kg/m²



Edge: B1
Perforation: Square 3x3mm holes, c/c 8.33mm in patterns
Perforation percent: 7.1 - 9.8% 
Surface: Unpainted cardboard
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low


Acoustics 
                  65mm suspension with 50mm mineral wool (M1F)

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.60
	0.65
	0.65
	0.60
	0.55
	0.65
	0.65


Installation
· c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.
· Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations. 

· Mount the furring crosswise the primary construction at a max c/c on 300mm.
· Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide. 
· Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.
· When filler is completely dry then sand with a fine sandpaper.

· Use a fine short-haired mohair roller to apply paint.
[image: image2.png]


Acoustical deck and wall mount panels 



Content          

Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
100% recyclable product.    

Products and materials


Globe_<900x2700> or < 1200x2400 > x 12.5_B1
Material: Perforated plasterboard

Board Type: Gypsum panel
Dimensions: <900x2700x12.5mm> or <1200x2400x12.5mm>

Weight: 9.20-9.90 kg/m²



Edge: B1
Perforation: Round 6mm holes, c/c 15mm in patterns
Perforation percent: 5.3 - 9.8%

Surface: Unpainted cardboard
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


65mm suspension with 50mm mineral wool (G1F)

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.35
	0.70
	0.80
	0.75
	0.60
	0.50
	0.65
	0.70


Installation
· c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.
· Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations. 

· Mount the furring crosswise the primary construction at a max c/c on 300mm.
· Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide. 
· Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.
· When filler is completely dry then sand with a fine sandpaper.

· Use a fine short-haired mohair roller to apply paint.
[image: image3.png]


Acoustical deck and wall mount panels 



Content          

Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
100% recyclable product.    

Products and materials


Quadril_<900x2700> or < 1200x2400 > x 12.5_B1
Material: Perforated plasterboard

Board Type: Gypsum panel
Dimensions: <900x2700x12.5mm> or <1200x2400x12.5mm>

Weight: 9.20-9.90 kg/m²



Edge: B1
Perforation:  Square 12x12mm holes, c/c 30mm in patterns
Perforation percent: 7.8 - 13%

Surface: Unpainted cardboard
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


65mm suspension with 50mm mineral wool (Q1F)

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.40
	0.65
	0.75
	0.70
	0.65
	0.50
	0.65
	0.70


Installation
· c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.
· Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations. 

· Mount the furring crosswise the primary construction at a max c/c on 300mm.
· Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide. 
· Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.
· When filler is completely dry then sand with a fine sandpaper.

· Use a fine short-haired mohair roller to apply paint.
[image: image4.png]


 Acoustical deck and wall mount panels 

Content          

Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
100% recyclable product.    

Products and materials

Tangent_900 x 2400 x 12.5_B1
Material: Perforated plasterboard

Board Type: Gypsum panel
Dimensions: 900 x 2400 x 12.5mm

Weight: 9.20-9.90 kg/m²



Edge: B1
Perforation: Obround 4x14mm holes, c/c 10/20mm in patterns
Perforation percent: 13.3 - 15%

Surface: Unpainted cardboard
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology


Acoustics 


65mm suspension with 50mm mineral wool (T3L1)

	125 Hz
	250 Hz
	500 Hz
	1000 Hz
	2000 Hz
	4000 Hz
	αw
	NRC

	0.35
	0.60
	0.70
	0.70
	0.65
	0.65
	0.70
	0.65


Installation
· c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.
· Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations. 

· Mount the furring crosswise the primary construction at a max c/c on 300mm.
· Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide. 
· Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.
· When filler is completely dry then sand with a fine sandpaper.

· Use a fine short-haired mohair roller to apply paint.
